Numerical simulations of damage and fracture in viscoelastic solids using a non-local fracture criterion

K. Sarah1, P. Thamburaja1,*, A. Srinivasa2, J.N. Reddy2

1 Department of Mechanical and Manufacturing Engineering, Universiti Kebangsaan Malaysia (UKM), Bangi 43600, Malaysia

2 Department of Mechanical Engineering, Texas A&M University (TAMU), College Station, TX 77843, USA

## Abstract

In this paper, we present a recently-developed three-dimensional finite-deformation rate form-based constitutive theory to describe the deformation and fracture of viscoelastic solids. The constitutive theory was also implemented into a commercial finite-element program through vectorized user-material subroutine. Damage and fracture in viscoelastic solids is simulated using the element failure (or element erosion) method coupled with a non-local fracture criterion which is based on the Gibbs free energy density. By numerically-simulating selected boundary value problems (BVPs), we show that our newly-developed computational framework for modeling fracture in viscoelastic solids is able to reproduce the correct stress-strain response, force-displacement response and crack propagation characteristics in viscoelastic solids undergoing fracture, when compared to the response obtained using the extended finite-element method (XFEM) implementation in a commercially-available finite-element program.

Keywords: Viscoelastic solid; Constitutive theory; Fracture; Finite-element method

* Corresponding author. Email address: p.thamburaja@ukm.edu.my (P. Thamburaja)